## Slide 1: Chiral magnetic Josephson junctions (Sup Spin)
18/07/2024
Justin Chen
art

## Slide 2: Motivation
Ability to tune stacks to create skyrmions leads to further development of skyrmionics devices
Seek to couple chiral magnetism with superconductivity via skyrmion-vortex pairs (SVPs)
Ferromagnet-insulator-superconductor (MIS) heterostructure (Andriyakhina 2021)
MFM image of SVP (Xie et. al 2023)

## Slide 3: Background

## Slide 4: Objectives
Simulate theoretical interaction of Skyrmion-Vortex pairs (SVPs).
Prepare and utilize instrumentation to efficiently analyze stacks and compare against simulated results.

## Slide 5: Results: Chiral Tilt Dependence, test
Did not record angles
But we see that tilt affects the gap

## Slide 6: Results: Chiral Tilt Dependence
No visible angle dependence, even if we consider angle magnitude
Signal too noisy

## Slide 7: Expectation: Co(0.9) vs Co(0.7)
Magnetic anisotropy and coercivity: As Co layer thickens, perpendicular magnetic anisotropy (PMA) might reduce, and coercivity increases. Larger coercivity might lead to smaller remanence, reducing RHE at low fields.
SOC and DMI: Strong SOC and DMI in thinner layers can lead to more complex spin textures and a larger RHE. Thicker Co layers can diminish these effects, leading to a smaller RHE
Magnetization and domain structure: Thinner layers generally exhibit more uniform magnetization and DW effects, leading to a larger RHE. Thicker layers can exhibit more complex DW structures and DW pinning, which can scatter electrons and reduce the RHE
Sample name | DW/Skyrmion type | Stack structure
FP2494 | Chiral Neel, DMI0 | Ir(1)/Fe(0.3)/Co(0.9)/Pt(1)
RAHE Paper | Chiral Neel, DMI0 | Ir(1)/Fe(0.3)/Co(0.7)/Pt(1)
Sample name | DW/Skyrmion type | Stack structure
FP2494 |  | Ir(1)/Fe(0.3)/Co(0.9)/Pt(1)
RAHE Paper |  | Ir(1)/Fe(0.3)/Co(0.7)/Pt(1)

## Slide 8: Expectation: Co(0.9) vs Co(0.7)
Magnetic anisotropy and coercivity: As Co layer thickens, perpendicular magnetic anisotropy (PMA) might reduce, and coercivity increases. Larger coercivity might lead to smaller remanence, reducing RHE at low fields.
SOC and DMI: Strong SOC and DMI in thinner layers can lead to more complex spin textures and a larger RHE. Thicker Co layers can diminish these effects, leading to a smaller RHE
Magnetization and domain structure: Thinner layers generally exhibit more uniform magnetization and DW effects, leading to a larger RHE. Thicker layers can exhibit more complex DW structures and DW pinning, which can scatter electrons and reduce the RHE
Therefore, we expect Fe(0.3)/Co(0.9) to have a smaller RHE
Sample name | DW/Skyrmion type | Stack structure
FP2494 | Chiral Neel, DMI0 | Ir(1)/Fe(0.3)/Co(0.9)/Pt(1)
RAHE Paper | Chiral Neel, DMI0 | Ir(1)/Fe(0.3)/Co(0.7)/Pt(1)
Sample name | DW/Skyrmion type | Stack structure
FP2494 |  | Ir(1)/Fe(0.3)/Co(0.9)/Pt(1)
RAHE Paper |  | Ir(1)/Fe(0.3)/Co(0.7)/Pt(1)

## Slide 9: Results: Co(0.9) vs Co(0.7)
We do indeed see that Co(0.9) has a smaller RHE %
Burgundy curve is between –ve and +ve curve, suggesting Gunasheel indeed adjusted to 0 deg tilt by eye

## Slide 10: Results: Achiral Tilt Dependence

## Slide 11: Comparison: Chiral + Achiral with similar MH curves
Sample name | DW/Skyrmion type | Stack structure
FP2494 | Chiral Neel, DMI0 | Ir(1)/Fe(0.3)/Co(0.9)/Pt(1)
FP2838 | Achiral Bloch, DMI=0 | Pt(1)/Co(2)/Pt(1)
Sample name | DW/Skyrmion type | Stack structure
FP2494 |  | Ir(1)/Fe(0.3)/Co(0.9)/Pt(1)
FP2838 | Achiral Bloch, DMI=0 | Pt(1)/Co(2)/Pt(1)
Remanence similar for both
Both have sheared hysteresis loop, but chiral has a skinnier sheared loops, which implies lower anisotropy

## Slide 12: Comparison: Chiral vs Achiral with similar MH curves
Sample name | DW/Skyrmion type | Stack structure
FP2494 | Chiral Neel, DMI0 | Ir(1)/Fe(0.3)/Co(0.9)/Pt(1)
FP2838 | Achiral Bloch, DMI=0 | Pt(1)/Co(2)/Pt(1)
Sample name | DW/Skyrmion type | Stack structure
FP2494 |  | Ir(1)/Fe(0.3)/Co(0.9)/Pt(1)
FP2838 | Achiral Bloch, DMI=0 | Pt(1)/Co(2)/Pt(1)
For RAHE paper, achiral RHE was larger than chiral RHE, for very different hysteresis loops
Here we achieve the same, but for similar hysteresis loops

## Slide 13: Future Work
Make new samples: Pt/Co/Pt, Ir/Fe/CoPt, and Ir/Co/Pt to have similar hysteresis and measure their RHE for Co thickness and tilt dependence
Remeasure Chiral sample to reduce noise and see if there’s any tilt dependence